PH12 - Photoluminescent Film

PRODUCT DESCRIPTION

Tape Technologies Photoluminescent Film (PH12) is a high performance photoluminescent film for signage. This film is rechargeable for “glow in the dark” signs. Photoluminescent absorbs visual lights and automatically glows in the dark for at least 12 hours once fully charged. It is dimensionally stable and offers excellent resistance to chemicals and stains.

No radioactive materials are used in the manufacturing of this product and it may be safely disposed of in a sanitary landfill.

PHYSICAL DESCRIPTION

| Face Film: | 12.5 mils film with a light yellow/green glossy appearance |
| --- | --- |
| Adhesive: | Permanent pressure sensitive adhesive |
| Release liner: | 75lb. White liner |
| Application Temperature: | 64ºF to 77ºF |
| Service Temperature: | -4ºF to 122ºF |
|  | FIGURES BELOW IN MILLICANDELA PER SQUARE METER |
| Candelas (mcd/m²) | 55.6 after 10 min 33.9 after 30 min 12.3 after 60 min 3.03 after 8 hours |

Shelf Life: One year when stored at temperature under 70ºF and 50% relative humidity,

protected from direct light.

APPLICATIONS, USES AND LIMITATIONS

Styletech Photoluminescent film is primarily intended for interior luminous labels, signs and markings.  It is not intended for application to complex curved, corrugated or riveted surfaces. It is not intended for surfaces subject to gasoline spills or vapors and is recommended for interior applications only.  The performance life may vary depending on application processes and techniques.  When properly processed and applied, this product will remain highly effective for up to 6 years.

ssc